| Leadhillite | Pb4(SO4)(CO3)2(OH)2 |
| --- | --- |
| Specimen from Granby MO | University of Cincinnati Mineral Collection (Click images to enlarge) |
|  | y |
|  | Transmitted light photomicrograph (Keyence VHX 600E) |
|  | Scanning Electron Microscope image (Hitachi ) |

| Crystal System | Specific gravity |  | Hardness | Color |  |
| --- | --- | --- | --- | --- | --- |
| Monoclinic | 6.4 |  | 2½ | Colorless, gray, yellow, white |  |
| Composition | Formula weight = 1078.90 g/mole |  |  |  |  |
| Pb | 76.82 % | PbO | 82.75 % |  |  |
| C | 2.23 | CO2 | 8.16 |  |  |
| O | 17.80 | H2O | 1.67 |  |  |
| S | 2.97 | SO3 | 7.42 |  |  |
| Web resources: | http://webmineral.com |  |  | http://www.mindat.org/ |  |

From the type locality, leadhill in Lanarkshire, Scotland

| Leadhillite in water distribution systems |  |
| --- | --- |
| Utility |  |
| Scanning Electron Microscope image (FEI XL 30 ESEM) | Scanning Electron Microscope image (FEI XL 30 ESEM) |