| Pyromorphite | Pb5(PO4)3X [X = Cl, F,or OH] |  |
| --- | --- | --- |
| Specimen from Yangshuo, Guangxi, China University of Cincinnati Mineral Collection |  | Specimen from unknown locality University of Cincinnati Mineral Collection (Click images to enlarge) |
| Reflected light photomicrograph | Scanning Electron Microscope image (FEI XL 30 ESEM) |  |

| Crystal System | Specific gravity | Hardness | Color |  |
| --- | --- | --- | --- | --- |
| Hexagonal | 6.85 | 3½ - 4 | Green, yellow, brown, grayish white |  |
| Composition | Formula weight = 1356.37 g/mole |  |  |  |
| Pb | 76.38 % | PbO | 82.2 % |  |
| O | 14.15 |  |  |  |
| P | 6.85 | P2O5 | 15.7 |  |
| Cl | 2.61 | Cl | 2.6 |  |
| Web resources: | http://webmineral.com |  | http://www.mindat.org/ |  |

From Greek for fire + form, in allusion to the apparent crystalline form it assume on cooling from fusion

| Pyromorphite in water distribution systems |  |
| --- | --- |
| Lead service branch, utility 01. Chloramine disinfection, phosphate corrosion control. | Scanning Electron Microscope image, utility 01 (FEI XL 30 ESEM) |
| Scanning Electron Microscope image, utility 01 (FEI XL 30 ESEM) | Scanning Electron Microscope image, utility 01 (FEI XL 30 ESEM) |