| Vanadinite | Pb5(VO4)3X [X = Cl, F,or OH] |
| --- | --- |
| Specimen from Mibladen, Morocco University of Cincinnati Mineral Collection | Specimen from Puzzler Mine, Yuma AZ (Click images to enlarge) |
| Scanning Electron Microscope image (FEI XL 30 ESEM) | Scanning Electron Microscope image (FEI XL 30 ESEM) |

| Crystal System | Specific gravity | Hardness | Color |  |
| --- | --- | --- | --- | --- |
| Tetragonal | 6.94 | 3½ - 4 | Brown, brownish yellow, brown, red, yellow, |  |
| Composition | Formula weight = 1416.27 g/mole |  |  |  |
| Pb | 73.15 % | PbO | 78.8 % |  |
| O | 13.56 |  |  |  |
| V | 10.79 | V2O5 | 19.26 |  |
| Cl | 2.50 | Cl | 2.5 |  |
| Web resources: | http://webmineral.com |  | http://www.mindat.org/ |  |

Name is an allusion to its composition

| Vanadinite in water distribution systems |  |
| --- | --- |
| Lead service branch, utility 20. Chloramine disinfection, phosphate corrosion control. | Scanning Electron Microscope image, utility 01 (Hitachi |
| Scanning Electron Microscope image, utility 20 (Hitachi | Scanning Electron Microscope image, utility 20 (FEI XL 30 ESEM) |